## Slide 1
Introduction
Ostrea rivularis Gould is one common oyster species with large consumption and wide popularity around the world, however, it is prone to spoilage due to its endogenous enzymes and microbial proliferation. Now, the application of active package is one effective way to maintain the quality of aquatic products.
Conclusions
This study verified that the shelf-life of oyster packaged by HPMC-FCD-CNE was extended to 4 days longer than the control group under 4℃ storage，indicating the obvious preservative and bacteriostatic functions of HPMC-FCD-CNE to oyster，, which can offer practical solutions for a better quality keeping and microbial control of Ostrea rivularis Gould under refrigeration.
Results
Method
The preparation of Citral Nanoemulsion and Composite Film.
Wrapped the shelled oysters with composite films and stored them at 4℃ (we set up four treatment groups, namely the Control, HPMC, HPMC-FCD, HPMC-FCD-CNE).
Assay of quality and microbial index (Sensory scores, K-value, TVB-N, TVC, and pH value).
Antibacterial mechanism (Nucleic acid and protein leakage, Growth curve, Bacterial live/dead staining).
Compare the shelf life of different groups of oysters through indicators.
Acknowledgements
This work was financially supported by Scientific Research Foundation of Hainan Tropical Ocean University (RHDRC202117 and RHDRC202307)
AIM
In this study, citral nanoemulsion (CNE) was prepared, and added into the composite film made by hydroxypropyl methylcellulose (HPMC) and fucoidin (FCD). The citral nanoemulsion composite film (HPMC-FCD-CNE) was utilized for quality preservation and control of microbial in Ostrea rivularis Gould under 4℃ storage, thereby extending their shelf-life.
References 1 PRADIZA R R et al. Study of tensile strength, microstructure and density-porosity properties of cassava starch-PLA bioplastic manufactured through solution casting[J/OL]. IOP Conference Series: Earth and Environmental Science, 2025, 1454(1): 012014.
2 KADER Md A et al. Development of biocompatible packaging material: starch/PVA-based bio-composite enhanced with hydroxypropyl methylcellulose[J/OL]. Polymer-Plastics Technology and Materials, 2024, 63(17): 2418-2432.
3 WANG L et al. Preparation of trilayer film with slow-release, antioxidant, and antibacterial activities and its effects on scallop preservation[J/OL]. Food Bioscience, 2024, 61: 104909.
4 HUANG Y et al. Effects of collagen‐based coating with chitosan and ε‐polylysine on sensory, texture, and biochemical changes of refrigerated Nemipterus virgatus fillets[J/OL]. Food Science & Nutrition, 2024, 12(3): 2145-2152.
The results showed that the HPMC-FCD-CNE had effective preservative and bacteriostatic properties, which was as indicated by changes in sensory score, total volatile base nitrogen (TVB-N), pH, K value, total viable count (TVC), and the colony number of specific spoilage organisms (SSOs). Compared to the control group without film package treatment, bacterial growth in oysters was significantly inhibited in all treatment groups by HPMC-FCD-CNE. Meanwhile, under the same storage day, the HPMC-FCD-CNE group showed higher sensory score, less TVB-N content and K value than other groups. The control group reached its shelf-life by day 10 (TVC: 7.383±0.250 lg CFU/g; TVB-N: 18.209 mg/100g; K value: 55.58%), while the HPMC-FCD-CNE group by day 14 (TVC: 7.787±0.076 lg CFU/g; TVB-N: 17.218 mg/100g; K value: 56.68%).
Fig 1. Antibacterial mechanism of composite film.
（A）Fluorescent staining observation of live/dead status； （B）TVC; (C) The colony number changes of Acinetobacter;
(D) The colony number changes of Pseudomonas； (E) Leakage of nucleic acids; (F) Leakage of proteins;
(G) Growth curves of Pseudomonas; (H) Growth curves of Pseudomonas Acinetobacter.
Preservative and bacteriostatic functions of citral nanoemulsion composite film on oyster during refrigeration
Fig 2. The quality changes of oysters under different treatment methods.
(I) Sensory scores; (J)K-value; (K)TVB-N; (L)pH
(The significant differences among different treatment groups within the same storage days are represented by a and b. The significant differences of the same treatment group among different storage days are represented by 1, 2.)
Contact Information:
liuguangyu622@gmail.com
Guangyu LIU1, Zhiheng HU2, Yaqin HU1
1 College of Food Science and Engineering, Yazhou Bay Innovation Institute, Hainan Tropical Ocean University, Marine Food Engineering Technology Research Center of Hainan Province, Collaborative Innovation Center of Marine Food Deep Processing, Hainan Key Laboratory of Herpetological Research, Sanya 572000, China
2 United Graduate School of Agricultural Sciences, Ueda 3-8-18, Morioka, Iwate 020-8550, Japan c Faculty of Agriculture, Iwate University, Ueda 3-8-18, Morioka, Iwate 020-8550, Japan
FSMILE 2025
October 04-07, 2025
@Morioka & ZOOM Cloud
International Symposium on Food Communications and Sustainable Agri-Aqua Food Systems
Connecting Primary Industries, Academia, and Society through the SDGs
A
B
C
D
E
F
G
H
pH
I
J
K
L